## Slide 1
Sohrab Ismail-Beigi
Applied Physics, Physics, Materials Science
Yale University
Describing exited electrons:
what, why, how,
and
what it has to do with charm++

## Slide 2: Density Functional Theory
For the ground-state of an interacting electron system we solve a Schrodinger-like equation for electrons
Hohenberg & Kohn, Phys. Rev. (1964); Kohn and Sham, Phys. Rev. (1965).
Approximations needed for Vxc(r) : LDA, GGA, etc.
Tempting: use these electron energies ϵj
to describe processes where
electrons change energy
(absorb light, current flow, etc.)

## Slide 3: DFT: problems with excitations
Material | LDA | Expt. [1]
Diamond | 3.9 | 5.48
Si | 0.5 | 1.17
LiCl | 6.0 | 9.4
Energy gaps (eV)
[1] Landolt-Bornstien, vol. III; Baldini & Bosacchi, Phys. Stat. Solidi (1970).
[2] Aspnes & Studna, Phys. Rev. B (1983)
Solar spectrum

## Slide 4: Green’s functions successes
Material | DFT-LDA | GW* | Expt.
Diamond | 3.9 | 5.6 | 5.48
Si | 0.5 | 1.3 | 1.17
LiCl | 6.0 | 9.1 | 9.4
Energy gaps (eV)
* Hybertsen & Louie, Phys. Rev. B (1986)
SiO2

## Slide 5: GW-BSE: what is it about?
DFT is a ground-state theory for electrons
But many processes involve exciting electrons:
Transport of electrons in a material or across an interface: dynamically adding an electron
e-

## Slide 6: GW-BSE: what is it about?
DFT is a ground-state theory for electrons
But many processes involve exciting electrons:
Transport of electrons in a material or across an interface: dynamically adding an electron
 The other electrons respond to this and modify energy of added electron
e-

## Slide 7: GW-BSE: what is it about?
DFT is a ground-state theory for electrons
But many processes involve exciting electrons:
Transport of electrons
Excited electrons: optical absorption promotes electron to higher energy
e-
h+

## Slide 8: Optical excitations
Single-particle view
  Photon absorbed
  one e- kicked into an empty state
Problem:
  e- & h+ are charged & interact
  their motion must be correlated
v
c
e-
h+
En
ħ

## Slide 9: Optical excitations: excitons
Exciton: correlated e--h+ pair excitation
Low-energy (bound) excitons: hydrogenic picture
Material | r (Å)
InP | 220
Si | 64
SiO2 | 4
Marder, Condensed Matter Physics (2000)
e-
h+
r

## Slide 10: GW-BSE: what is it about?
DFT is a ground-state theory for electrons
But many processes involve exciting electrons:
Transport of electrons
Excited electrons: optical absorption promotes electron to higher energy
 The missing electron (hole) has + charge, attracts electron:
modifies excitation energy and absorption strength
e-
h+

## Slide 11: GW-BSE: what is it about?
DFT is a ground-state theory for electrons
But many processes involve exciting electrons:
Transport of electrons, electron energy levels
Excited electrons
Each/both critical in many materials problems, e.g.
Photovoltaics
Photochemistry
“Ordinary” chemistry involving electron transfer

## Slide 12: GW-BSE: what is it for?
DFT is a ground-state theory for electrons
But many processes involve exciting electrons:
Transport of electrons, electron energy levels
Excited electrons
DFT --- in principle and in practice --- does a poor job of describing both
GW : describe added electron energies including response of other electrons
BSE (Bethe-Salpeter Equation): describe optical processes including electron-hole interaction and GW energies

## Slide 13: A system I’d love to do GW-BSE on…
Zinc oxide nanowire
P3HT polymer
But with available GW-BSE methods
it would take “forever”
i.e. use up all my supercomputer allocation time

## Slide 14: GW-BSE is expensive
Scaling with number of atoms N
DFT : N3
GW : N4
BSE : N6

## Slide 15: GW-BSE is expensive
Scaling with number of atoms N
DFT : N3
GW : N4
BSE : N6
But in practice the GW is the killer
e.g. a system with 50-75 atoms (GaN)
DFT : 1 cpu x hours
GW : 91 cpu x hours
BSE : 2 cpu x hours

## Slide 16: GW-BSE is expensive
Scaling with number of atoms N
DFT : N3
GW : N4
BSE : N6
But in practice the GW is the killer
e.g. a system with 50-75 atoms (GaN)
DFT : 1 cpu x hours
GW : 91 cpu x hours
BSE : 2 cpu x hours
Hence, our first focus is on GW
Once that is scaling well, we will attack the BSE

## Slide 17: What’s in the GW?
Key element : compute response of electrons to perturbation
P(r,r’) = Response of electron density n(r) at position r to change of potential V(r’) at position r’
Notes: The factor fi=1 if a state if filled with electron and 0 if empty in the ground state. The sum over j this in theory goes to infinity

## Slide 18: What’s in the GW?
Key element : compute response of electrons to perturbation
P(r,r’) = Response of electron density n(r) at position r to change of potential V(r’) at position r’
Challenges
Many FFTs to get wave functions 𝜓i(r) functions
Large outer product to form P
Dense r grid : P(r,r’) is huge in memory
Sum over j is very large
Notes: The factor fi=1 if a state if filled with electron and 0 if empty in the ground state. The sum over j this in theory goes to infinity

## Slide 19: What’s in the GW?
Key element : compute response of electrons to perturbation
P(r,r’) = Response of electron density n(r) at position r to change of potential V(r’) at position r’
Challenges
Many FFTs to get wave functions 𝜓i(r) functions
Large outer product to form P
Dense r grid : P(r,r’) is huge in memory
Sum over j is very large
1 & 2 : Efficient parallel FFTs and linear algebra
3 : Effective memory parallelization
4 : replace explicit j sum by implicit inversion (many matrix-vector multiplies)
Notes: The factor fi=1 if a state if filled with electron and 0 if empty in the ground state. The sum over j this in theory goes to infinity

## Slide 20: Summary
GW-BSE is promising as it contains the right physics
Very expensive : computation and memory
Plan to implement high performance version in OpenAtom for the community (SI2-SSI NSF grant)
Two sets of challenges
How to best parallelize existing GW-BSE algorithms? Will rely on Charm++ to deliver high performance Coding, maintenance, migration to other computers much easier for user
Need to improve GW-BSE algorithms to use the computers more effective (theoretical physicist/chemist’s job)

## Slide 22: One particle Green’s function
(r’,0)
(r,t)
Dyson Equation:
DFT:
Hedin, Phys. Rev. (1965); Hybertsen & Louie, Phys. Rev. B (1986).

## Slide 23: Two particle Green’s function
(r’’’,0)
(r,t)
(r’,t)
(r’’,0)
Exciton amplitude:
Bethe-Salpeter Equation:
(BSE)
v
c
e-
h+
attractive
(screened direct)
repulsive
(exchange)
Rohlfing & Louie; Albrecht et al.; Benedict et al.: PRL (1998)

## Slide 24: STE geometry
Si1
Si2
O1
Bond (Å) | Bulk | STE
Si1-O1 | 1.60 | 1.97 (+23%)
Si2-O1 | 1.60 | 1.68 (+5%)
Si1-Oother | 1.60 | 1.66 (+4%)
Angles | Bulk | STE
O1-Si1-Oother | 109o | ≈ 85o
Oother-Si1-Oother | 109o | ≈ 120o
Prob : 20,40,60,80% max

## Slide 25: Exciton self-trapping
Defects  localized states: exciton can get trapped
Interesting case: self-trapping
If exciton in ideal crystal can lower its energy by localizing
defect forms spontaneously
 traps exciton
e-
h+
h+
e-